## Slide 1: Catalytic degradation of Natural Organic Matter (NOM) by Advanced Oxidation Technologies
1 Research Group on Functional Materials and Catalysis (GIMFC), Nariño University, Department of Chemistry, Colombia
2 Research Group on Environmental Remediation and Biocatalysis, Antioquia University, Colombia
3 Salamanca University Department of Inorganic Chemistry, Spain
4 Public University of Navarre, Campus Arrosadía, Spain
Ana María García1,*, Ricardo A. Torres-Palma2, Miguel-Ángel Vicente3, Antonio Gil4 and Luis-Alejandro Galeano1,*
(*) Presenting Author’s E-mail: ana.garcia11@udea.edu.co
(*) Corresponding Author´s E-mail: alejandrogaleano@udenar.edu.co

## Slide 2: INTRODUCTION

## Slide 3
NOM composition
Humic acids (HA)
Fulvic acids (FA)
humins
Leenheer et al. (2003). Sci. Technol. 37, 18A–26A.
3

## Slide 4
Chemical composition and molecular size
Functional groups, including esteric, phenolic, quinine, carboxylic, hydroxyl, amino, and nitroso compounds.
Molecular weight
From several hundreds to tens of thousands (Humic substances).
Structure
Substituted aromatic rings linked to aliphatic chains.
4
Property | HA | FA
Elemental composition (Weight %) |  | 
Carbon | 50–60 | 40–50
Hydrogen | 4–6 | 4–6
Oxygen | 30–35 | 44–50
Nitrogen | 2–4 | <1–3
Sulfur | 1–2 | 0–2
Solubility below pH 2.0 | Not soluble | Soluble
Apparent molecular weight range (atomic mass units) | Few hundreds to several millions | 180–10,000
Functional group distribution |  | 
Carboxyl (–COOH) | 14–45 | 58–65
Phenol (–Ph) | 10–38 | 9–19
Alcohol (–R–OH) | 13–15 | 11–16
Carbonyl (–C=O) | 4–23 | 4–11
Methoxyl (–O–CH3) | 1–5 | 1–2
Matilainen et al. (2011). Chemosphere 83, 1431–1442.
NOM composition

## Slide 5
Some other aspects to take into account….
5
Saturation of activated carbon
Fouling of membranes
Substrate for bacterial growth
Gough et al. (2014). Sci. Total Environ. 468–469, 228–239.
Cl2
NOM
DBPs
Trihalomethanes
THMs
Haloacetic acids
HAAs
700 DBPs
color
taste
odor

## Slide 6
Typical NOM concentrations in real water sources
6
Chart: 
| HPO | HPI | TPI
% | 36 | 32 | 25
Chart: 
| HPO | HPI | TPI
% | 30 | 28 | 19
Chart: 
| HPO | HPI
% | 60 | 40
Chart: 
| HPO | HPI
% | 65 | 40
Effluent of wastewater treatment plant
Effluent of aeration followed by activated sludge
Secondary effluent from a water regeneration plant
Effluent of pre-treatment with activated sludge, coagulation and sand filtration
Wastewater 20
Surface water: 2 - 20
Groundwater: 0.5 – 2.0
Gong et al. (2008). Water Res. 42, 1238-1244.
Jarusutthirak et al. (2002). Desalination 145, 247-255..
Hu et al. (2003). Water Res. 37, 4801-4809.
Zhang et al. (2009) J. Hazard. Mater. 164, 1433-1438
HPI: Hydrophilic fraction
HPO: Hydrophobic fraction
TPI: Transphilic fraction
TOC (mg/L)

## Slide 7
7
Typical treatment stages at drinking water facilities
Dist.
Sys.
Clear
well
Coagulant
Disinfectant
Settling
Corrosion Control
Fluoride
raw water
flocculation
rapid
mix
Filtration
Remove some of the NOM & suspended particles
Kills or inactivates pathogenic organisms

## Slide 8
8
AOTs
HO•
H2O2/Fe3+ (Fenton - like)
H2O2/Fe2+ (Fe3+) /UV (Photoassisted Fenton)
H2O2/Fe3+- oxalate
Mn2+/Oxalic acid/O3
TiO2/hn/O2 Photocatalytic
O3/H2O2
O3/UV
H2O2/UV
H2O2/Fe2+ (Fenton)
CWPO
Fe,Cu-catalysts
CO2 + H2O and by-products
+ H2O2
MINERALIZATION
HO. Eº = 2,80
GOAL
NOM

## Slide 9: 2. AOTs FOR NOM DEGRADATION
O H
O H
O H
O H
O H

## Slide 10
Global interest in AOTs for catalytic degradation of NOM in the past few years
10
Figure 1. Number of publications in indexed journals containing the following keywords: NOM: natural organic matter; AOPs: advanced process oxidation; DW: drinking water; WW: wastewater in abstract through 2006 to 2016.
Source: Scopus, October 30, 2016.
AOTs+NOM+DW
AOTs+NOM
AOTs+WW

## Slide 11
11
UV-light based degradation
Goslan et al. (2006). Chemosphere 65, 1113–1119.
Figure 2. Treatment of reservoir water by UV-C photolysis (initial
DOC = 17.4 mg L-1, initial UV254 = 53.58 m-1).
UVC < UV/H2O2
Target compound
NOM
Matrix
Raw water, [DOC]0 = 17.4 mg/L, UV254=53.58 m-1, pH: 4.54
AOT features
UV lamp at 254 nm
Recorded parameters
DOC, UV254, HP-SEC

## Slide 12
12
UV-light based degradation
Goslan et al. (2006). Chemosphere 65, 1113–1119.
Figure 2. Treatment of reservoir water by UV-C photolysis (initial
DOC = 17.4 mg L-1, initial UV254 = 53.58 m-1).
UVC < UVC/H2O2
Figure 3. HP-SEC molecular size distribution of reservoir water treated at optimum reaction conditions for each process

## Slide 13
13
Fenton processes: photo-Fenton
Target compound
HA
Matrix
Synthetic HA solution (Fluka
HA)
AOT features
Fenton reagent/UVA with máximum centered at 365 nm
Recorded parameters
DOC, UV254, HP-SEC, LCC
fractionation
Figure 4. Removal of UV254 at different H2O2 to Fe3+ molar ratios
Sanly et al. (2007). Sep. Sci. Technol. 42, 1391–1404.
UVA/Fe3+
UVA/Fe3+:H2O2(1:1)
UVA/Fe3+:H2O2(1:5)
UVA/H2O2
UVA/Fe3+:H2O2(1:15)

## Slide 14
14
Fenton heterogeneous processes: Al/Fe-PILC activated
Galeano et al. (2012). Appl. Catal. B: Environ. 111-112, 527-535.
Catalytic Wet Peroxide Oxidation (CWPO)

## Slide 15
15
Catalytic Wet Peroxide Oxidation (CWPO): color removal
[Fe]leach. ≤ 0.5 mg/dm3
Target compound
NOM
Matrix
Surface water, [COD]0 = 40.14 mg O2/dm3
[Color455]0 = 42 PCU
AOP features
[Catalyst] = 0.5 g/dm3
[H2O2]ad. = 0.047 mol/dm3
H2O2 veloc. = 6.0 cm3/h
[H2O2]/[COD]0 = 1.0
pH = 3.7
T = 291 ± 2.0 K
P = 72 kPa
Recorded parameters
COD, Color removal
Galeano et al. (2012). Appl. Catal. B: Environ. 111-112, 527-535.
PCU: Pt-Co units
Figure 5. Color455 removals from raw surface water displayed by the clay catalysts.

## Slide 16
16
Photocatalysis
Target compound
NOM
Matrix
Surface water, [DOC]0 = 2 mg/L, UV254=0.081 cm-1, pH: 6.5
AOT features
Degussa Cu/TiO2
Recorded parameters
SEC, DOC
Figure 6. Control experiments for the inhibiting effect of added Cu2+.
Espinoza et al. (2011). Water Res. 45, 1039–1048.
Photon
VB
CB
Band gap

## Slide 17
17
Target compound
HA
Matrix
Surface water, , TOC0=16.2 mg/L
AOT features
Anode: Pt or BDD, Cathode: CS o SS, pH 3.0, EF: 0.1 mM Fe2+
Recorded parameters
TOCtot= TOCsol + TOCads
UV-vis
ICP-OES: [Fe]
Electro-Fenton (EF) and anodic oxidation (AO)
Trellú et al. (2016). Appl. Catal. B: Environ. 194, 32-41
Figura 7. Scheme of removal of humic acids from drinking water by anodic oxidation and electro-Fenton processes.

## Slide 18
18
Electro-Fenton (EF) and anodic oxidation (AO)
Target compound
HA
Matrix
Surface water, , TOC0=16.2 mg/L
AOT features
Anode: Pt or BDD, Cathode: CS, pH 3.0, EF: 0.1 mM Fe2+
Recorded parameters
TOCtot= TOCsol + TOCads
UV-vis
ICP-OES: [Fe]
EF-Pt
Figure 8. Evolution of TOCsol and TOCads during the electrolysis of HAs solution (TOC0= 16.2 mg L−1) by EF-Pt process at 300 mA (0.05 M Na2SO4; 0.1 mM Fe2+). Symbols report experimental results. Error bars refer to triplicate experiments. Lines report model results.
40 min, Promotes sorption: complexation HAs + Fe
Trellú et al. (2016). Appl. Catal. B: Environ. 194, 32-41
38 %
85 %

## Slide 19: THANK YOU