## Slide 1
Statistical optimization of the catalytic wet peroxide oxidation (CWPO) of phenol activated by Al/Fe-PILC clay catalyst
Luis Alejandro Galeano1; Jessica Basante
1 Grupo de Investigación en Materiales Funcionales y Catálisis (GIMFC) Departamento de Química, Universidad de Nariño. Pasto – Colombia.
E-mail: alejandrogaleano@udenar.edu.co

## Slide 2
Introduction

## Slide 3: Advanced Oxidation Processes (AOPs)
HO·
H2O2/Fe2+ (Fenton)
H2O2/Fe3+ (Fenton - like)
H2O2/Fe2+ (Fe3+)/UV (Photo-assisted Fenton)
H2O2/Fe3+- oxalate
Mn2+/Oxalic acid/O3
TiO2/hn/O2 Photo -catalytic
O3/H2O2
O3/UV
H2O2/UV
CWPO
Fe,Cu – solid catalysts

## Slide 4: Al/Fe Pillared clays (Al/Fe-PILCs) useful catalyzing CWPO
Al2O3 Pillar
Mixed Al/Fe pillar
Fe decorating
Al2O3 pillar
Cluster AlxOy
Cluster FexOy
SBET
d001
T stability
Accesibility
Catalytic performance
Galeano, L. A.; Gil, A.; Vicente, M. A. Appl. Catal. B-Environ. 100 (1) (2010) 271-281.
Notes: Arcillas porqué? Accesibilidad, bajo costo
Refinación previa encarece el proceso!
Propiedades microporosas.

## Slide 5
Al/Fe-PILC
Drinking Water
CWPO
CWPO – Drinking Water
Catalyst shaping
Extrudates
Microspheres
Simpler and efficient clay Interlayering method
Al/Fe-PILC
Efficient CWPO active catalyst
Catalytic potential
MO; PhO; NOM
Highly concentrated Interlayering Al/Fe mixed hydrolyzed precursor
Scaling-up
[Al(Al12O4(OH)24(OH2)12]7+
d001
Fe uptake!
Intensification process

## Slide 6
CWPO
[subst.]
pH
Catal. nature
[Catal.]
[H2O2]
T
P
Etc….
[PhO]
pH
[Catal]
[H2O2]
Factors affecting catalytic performance in CWPO reaction

## Slide 7
One factor at a time….
Minimum number of experiments
DOE/RSM
Montgomery D.C., (2005). Design and Analysis of Experiments, 6th. ed., John Wiley & Sons, Inc.
Statistically significant results

## Slide 8
Experimental

## Slide 9
Experimental design for optimization of the main operating parameters in the CWPO degradation of phenol (PhO) under variable physicochemical characteristics
Central Composite Factorial 22
experimental design
Experimental factors: 2
Number of blocks: 1
Number of runs: 10
Hydrogen Peroxide dose (%):
55.0 – 75.0
Catalyst concentration
(g/L): 1.5 - 4.0
Non-controlable variables
pH0
6.0 – 9.0
Starting PhO concentration [PhO]0
TOC (mg C/L): 2.0 – 20.0
Temperature of reaction (Tr) (°C): 5.0 – 25.0
Semi-batch reactor
Reaction time: 180 min
GOALS:
Minimum TOC
máximum PhO degradation.
maximum fraction of H2O2 reacted
Responses: 3
PhO mineralization TOC removal (%)
[H2O2]r (%) (Spectrophotometric)
PhO Removal (%) - HPLC
[Al/Fe-PILC]
0.62 % Feactive

## Slide 10
Results

## Slide 11
Exp | Factors |  | Responses |  |  | Co-variables |  |  | [Feact.]/[H2O2]
 | H2O2 dosing (Stoic. %) | [CAT] (g/L) | TOC removal (%/g cat.) | H2O2 React. (%/g Cat.)d | PhOdegr. (%/g Cat.) | pH0 | TOC0 (mg/L) | T (°C) | 
1 | 65.0 (50.6) | 2.750 | 11.923 | 14.962 | 11.359 | 7.2 | 12.0 (15.4) | 22.6 | 0.070
2 | 72.1 (68.7) | 3.634 | 8.120 | 17.548 | 9.373 | 8.9 | 7.7 (8.0) | 12.3 | 0.131
3 | 75.0 (62.7) | 2.750 | 11.722 | 20.295 | 15.834 | 6.7 | 10.7 (12.8) | 6.1 | 0.068
4 | 72.1 (64.7) | 1.866 | 15.335 | 33.255 | 23.362 | 7.2 | 9.0 (10.0) | 10.0 | 0.057
5 | 55.0 (52.9) | 2.750 | 18.960 | 37.204 | 14.776 | 7.5 | 11.5 (12.0) | 15.1 | 0.086
6 | 57.9 (58.0) | 1.866 | 27.759 | 41.713 | 24.759 | 6.7 | 14.6 (14.6) | 21.0 | 0.044
7 | 65.0 (59.1) | 4.000 | 14.935 | 12.969 | 10.903 | 7.1 | 18.6 (20.4) | 25.6 | 0.065
8 | 65.0 (60.2) | 2.750 | 11.983 | 18.211 | 14.023 | 7.0 | 5.8 (6.3) | 17.6 | 0.144
9 | 65.0 (61.0) | 1.500 | 27.045 | 46.668 | 24.899 | 7.0 | 14.9 (15.9) | 23.3 | 0.031
10 | 57.9 (53.6) | 3.634 | 11.219 | 16.165 | 10.021 | 6.9 | 10.5 (11.4) | 19.2 | 0.118
Matrix of experiments

## Slide 12
Statistical significance of every response
PhO degr.
TOC removal
H2O2 reacted

## Slide 13
Single-response surfaces
Response | Optimal value (%/g cat.) | Factor | 
 |  | H2O2 dosing (Stoic. %) | [CAT] (g/L)
PhOdegr. | 29.4 | 75.0 | 1.5
TOC removal | 36,4 | 55.0 | 1.5
H2O2 React. | 65,7 | 55.0 | 1.5

## Slide 14
Combined, multi-response surface in semi-batch reactor
Response | Optimal value (%/g cat.) | Factor | 
 |  | H2O2 dosing (Stoic. %) | [CAT] (g/L)
PhOdegr. | 19.8 | 62.0 | 1.5
TOC removal | 30.0 |  | 
H2O2 React. | 26.9 |  | 

## Slide 15
Combined, multi-response surface in slurry continuous reactor
Optimized multiple-response surface (desirability function: maximized [TOC]r and [PDL]r and minimized [H2O2]r) of the CWHPO degradation of phenol by Al/Fe-PILC catalyst in continuous slurry reactor
Ramírez, J.H.; Galeano L.A. et al. J. Environ. Chem. Eng. (2017) submitted.

## Slide 16
Optimal conditions translated to continuous slurry reactor
Reaction volume 1.3 dm3; T = 18.0 +/- 1.0 °C; atmospheric pressure = 76 kPa; pH = 7.0; stirring rate 600 rpm; Qphenol = 8.0 mL/min; [Phenol]in = 0.276 mmol/L ([TOC]in = 20 mg C/L); QH2O2 = 1.6 mL/min; [H2O2]in = 20.91 mmol/L; [Al/Fe-PILC] = 1.77 g/L and residence time = 135 minutes.
Ramírez, J.H.; Galeano L.A. et al. J. Environ. Chem. Eng. (2017) submitted.

## Slide 17: Concluding Remarks
Statistical RSM is useful tool optimizing heterogeneous Fenton degradation of contaminants in water samples displaying varied physicochemical characteristics.
Optimal CWPO degradation of phenol under circumneutral pH conditions decreases significantly either, the top pollutant’s degradation, TOC removal and use of hydrogen peroxide respect to performance at pH values < 4.0.
Use of responses defined per gram of catalyst enabled successful optimización in semi-batch reactor (adsorption disregarded).