## Slide 1
[Al/Fe-PILC] (g/dm3)
Desirability
Desirability
[H2O2]d (%)
RSM optimization of natural organic matter degradation by Catalytic Wet Peroxide Oxidation
3rd Iberoamerican Conference on Advanced Oxidation Technologies (III CIPOA)
2nd Colombian Conference on Advanced Oxidation Processes (II Ccpaox)
November 14 – 17, 2017
Medellín (Guatapé), Colombia
A.M. Garcia-Mora1,2, R. Torres-Palma2, L.A.Galeano1.
(1) Grupo de Investigación en Materiales Funcionales y Catálisis, Departamento de Química, Universidad de Nariño, Calle 18, Cra 50 Campus Torobajo, Pasto, Colombia, Email: anamariagarcia@udenar.edu.co; ana.garcia11@udea.edu.co
(2) Grupo de Investigación en Remediación Ambiental y Biocatálisis, Instituto de Química, Facultad de Ciencias Exactas y Naturales, Universidad de Antioquia UdeA, Calle 70 No. 52-21, Medellín, Colombia.
Results
H2O2/Fe3+ (Fenton - like)
CWPO
Fe,Cu-catalysts
HO. Eº = 2.80 V
NOM-mineral
interface
–NOM
–NOMads
H2O2(aq)
HO•+HO2•
Mixed pillar Al/Fe
Al/Fe-pillared clay catalyst
Methodology
Table 1. Preparation of synthetic NOM surrogate based on standards of different polarity.
Reagent1 |  | NOM-fraction modelled2 | Molecular weight (Da) | Abundance in synthetic water (TOC %)
Polyacrylic acid (PAA) |  | TPI | 130.000 | 20
Polystyrene sulfonate (PSS) | PSS-1 | HPO | 1´000.000 | 12.5
 | PSS-2 | HPO | 200.000 | 12.5
Polygalacturonic acid (PGUA) |  | HPI | 25.000-50.000 | 30
Humic acids (HA) |  | HPO | - | 25
Fig. 1 Preparation of synthetic water
1All reagents Sigma-Aldrich used as received
2HPI: hydrophilic; TPI: transphilic; HPO: hydrophobic
Fig. 2 Relationships between three most influencing CWPO factors.
Type of design | 23
Optimization type | Central Composite
Number of runs | 10
Fig. 3 Real laboratory set-up for CWPO-degradation of NOM. Experimental parameters: Peroxide Dose [H2O2]d= 13.1 % stoichiometric (SW: 87 mg/L, RW: 50 mg/L); Catalyst concentration [Al/Fe-PILC]*: 6.0 g/dm3; pHSW 7.0 and pHRW 7.3; TemperatureSW: 25 °C and TemperatureRW: 14 °C (RT on sampling); full reaction time: 180 min; full recorded time: 240 min.
Synthetic water
H2O2
pH control
air bubbling
NOM
+
C2-Exp-PILC
Sample
T control
H2O2
sampling
Mechanical stirring
zoom
T control
% Stoichiometric dose: 7.08 mg H2O2/mg COT [1]
Analytical methods
Fig. 4 Spectrophotometer UV-2600
* Al/Fe-PILC: Atomic Metal Ratio AMR (Fe) = 3.17 %; Total Metal Concentration (TMC) = 5.73 mol/dm3; Interlayering solution: Auto-hydrolysis with starting ratio (Al3+/Al0) = 14/86 [2]; Final heating: 400 °C/2 h). Final Feactive content: 0.62 wt. %.
Fig. 5 Dissolved organic carbon.
Table 2. First and second experimental designs (DOEs) used to optimize main operating parameters of CWPO.
Introduction
DOE1-NOM
NOM decolourization
(%) (Spectrophotometric)
H2O2 reacted: [H2O2]r (%) (Spectrophotometric)
NOM mineralization TOC removal (%)
Optimization
Optimal response
Goal: maximize all responses
[Al/Fe-PILC] (g/dm3)
Desirability
Desirability
[H2O2]d (%)
Desirability: NOM decolourization + [H2O2 ]r + NOM mineralization
Fig. 6 Response surface for NOM mineralization (TOC removal).
Fig. 8 Multivariate Response surface – Desirability DOE1-NOM.
Fig. 7 Pareto’s diagram for TOC removal.
B: [Al/Fe-PILC]
A: [H2O2]d
Optimized desirability = 0.97
[Al/Fe-PILC]optimal = 6.01 g/dm3
[H2O2]d optimal = 7.72 %
TOC removal
[Al/Fe-PILC] (g/dm3)
[H2O2]d (%)
TOC removal
DOE2-NOM
Fig. 9 Multivariate Response surface – Desirability DOE2-NOM.
Optimized desirability = 0.85
[Al/Fe-PILC]optimal = 6.0 g/dm3
[H2O2]d optimal = 13.1 %
2.432 mmol Fe/mmol H2O2 added
[Al/Fe-PILC]
p-value: 0.0184
B: [Al/Fe-PILC]
A: [H2O2]d
H2O2 Dose
p-value: 0.0375
A: [H2O2]d
B: [Al/Fe-PILC]
Fig. 10 Pareto’s diagram for H2O2 reacted.
Fig. 11 Pareto’s diagram for NOM removal.
Fig. 12 CWPO degradation of NOM: organic color removed at 456 nm (2120C-Standard Methods) and DOC mineralization (TOC-L Analyzer Shimadzu) to Synthetic and raw water*.
Fig. 13 Fraction of hydrogen peroxide reacted vs. added through the CWPO catalytic tests.
* Raw water collected in Vereda Charandú surface source. Surrounding of Ipiales – Nariño, Colombia
Acknowledgment
Financial support from CWPO for enhanced Drinking Water Quality in Nariño Project (BPIN 2014000100020), CT&I Fund of the SGR – Colombia is gratefully acknowledged. AMG also thanks PhD Scholarship granted From Nariño Department Program (BPIN 2013000100092).
References
[1] Deng Y., Englehardt J., Water Res. 40 (2006), 3683– 3694.
[2] Akitt W. J, Farthing A., J. Chem. Soc., Dalton Trans. (1981), 1624-1628.
[3] Galeano L.A., Bravo P.F., Luna C.D., Vicente M.A, Gil A., App. Catal. B 111–112 (2012), 527-535.
The removal of natural organic matter from aqueous solutions using Catalytic Wet Peroxide Oxidation activated by Al/Fe-PILC catalyst was successfully optimized by using statistical tools. Optimal operating conditions at neutral starting pH were found to be: [H2O2]d 13.1 %; [Al/Fe-PILC] 6.0 g/L within a range of starting TOC concentrations (0 – 20 mg C/L) and controlled temperatures (5.0 - 25 °C). Catalytic tests under optimal conditions achieved higher percentage of color removal (~ 93 %) on raw water than on synthetic water (~ 50 %); however, NOM mineralization was significantly higher (75 %) on synthetic water vs. real water (37 %), probably because of formation of more refractory hydrophilic substances along process on real water.
Conclusions
NOM: Natural organic matter
CWPO: Catalytic wet peroxide oxidation