## Slide 1: Optimization of Methyl Orange’s Catalytic Wet Peroxide Oxidation (CWPO) by the Response Surface Methodology
Luis Alejandro GALEANO1,*, Viviana N. AGUILAR1, Miguel A. VICENTE2 and Antonio GIL3
1 Research Group on Functional Materials and Catalysis (GIMFC), Department of Chemistry, University of Nariño. Calle 18 Cra. 50, Campus Torobajo, Pasto – Colombia.
2 Department of Inorganic Chemistry, Chemical Sciences Faculty, Salamanca University. Plaza de la Merced, s/n, Salamanca, 37008. Spain.
3 Department of Applied Chemistry, Public University of Navarra. Edificio Los Acebos, Campus de Arrosadía, Pamplona, 31006. Spain.
(*) Corresponding author: alejandrogaleano@udenar.edu.co

## Slide 2: INTRODUCTION

## Slide 3: Advanced Oxidation Processes (AOPs)
HO·
H2O2/Fe2+ (Fenton)
H2O2/Fe3+ (Fenton - like)
H2O2/Fe2+ (Fe3+) /UV (Photoassisted Fenton)
H2O2/Fe3+- oxalate
Mn2+/Oxalic acid/O3
TiO2/hn/O2 Photocatalytic
O3/H2O2
O3/UV
H2O2/UV
CWPO
Fe,Cu – bearing solid catalysts

## Slide 4
Al2O3 - Pillar
Al/Fe mixed pillar
Fe “decorated”
Al2O3 - pillar
Al Cluster
Fe cluster
SBET
T stability
Catalytic activity

## Slide 5: Catalytic Wet Peroxide Oxidation (CWPO) of MO
H2O2
HO. + HO.2
CO2 + NO3- + SO42- + H2O
Galeano et al. (2010). Appl. Catal. B: Environ. 100, 271-281.
(MO)

## Slide 6
CWPO
[subst.]
pH
Catal. nature
[Catal.]
[H2O2]
T
P
Etc….
[MO]
pH
[Catal.]
[H2O2]
Factors affecting catalytic assessment in CWPO reaction

## Slide 7
One factor at a time….
Statistically significant results
Minimum number of experiments
DOE/RSM
Montgomery D.C., (2005). Design and Analysis of Experiments, 6th. ed., John Wiley & Sons, Inc.

## Slide 8: Materials and methods

## Slide 9
250 cm3 MO (sln)
+ powdered
catalyst
H2O2 addition
pH control:
NaOH (sln.) 0.2 M
H2SO4 (sln.) 0.2 M
Sampling
(4 h)
Catalytic test
Air bubbling (CO2 displacement)

## Slide 10
FACTOR | Low level (-1) | High level (+1)
pH | 3.7 | 7
[H2O2] (mol/L) | 0.0685* | 1.0964**
[MO] (mg/L) | 50 | 200
[CAT] (g/L) | 0.5 | 5.0
Table 1. Chosen levels for every factor in the experimental design
Type of design: 24 factorial design
Number of runs: 16
Response parameters: MO elimination
[H2O2]rem.
Experimental Design – CWPO optimization
* It corresponds to 50 % of the theoretical dosage required for full mineralization.
** It corresponds to 200 % of the theoretical dosage required for full mineralization.
Statgraphics ® Centurion XVI professional statistical package was used for analyses.

## Slide 11: results

## Slide 12
Source | Sum of Squares |  | FD | Mean Square | F | P-value
A: [CAT] | 178.289 | 1 |  | 178.289 | 7.45 | 0.0413
B: pH | 46.6831 | 1 |  | 46.6831 | 1.95 | 0.2213
C: [MO] | 46.7514 | 1 |  | 46.7514 | 1.95 | 0.2210
D: [H2O2] | 1104.07 | 1 |  | 1104.07 | 46.14 | 0.0011
AB | 124.267 | 1 |  | 124.267 | 5.19 | 0.0716
AC | 133.807 | 1 |  | 133.807 | 5.59 | 0.0644
AD | 72.5478 | 1 |  | 72.5478 | 3.03 | 0.1421
BC | 399.3 | 1 |  | 399.3 | 16.69 | 0.0095
BD | 18.5977 | 1 |  | 18.5977 | 0.78 | 0.4183
CD | 15.1516 | 1 |  | 15.1516 | 0.63 | 0.4623
Error total | 119.632 | 5 |  | 23.9264 |  | 
Total (corr.) | 2259.09 | 15 |  |  |  | 
Statistical analysis for response parameter MO elimination (%)
Table 2. Analysis of variance for MO elimination (%)

## Slide 13
Figure 1. Pareto’s diagram for MO elimination (%)
[H2O2]
BC
A: [CAT]
AC
AB
AD
C: [MO]
B: pH
BD
CD
Standardized effect

## Slide 14
(a)
(b)
(c)
(d)
(e)
(f)
Figure 2. Surface diagrams for the response MO elimination (%)

## Slide 15
Source | Sum of Squares | FD | Mean Square | F | P-value
A:[CAT] | 0,600625 | 1 | 0,600625 | 0,74 | 0,4297
B:pH | 0,25 | 1 | 0,25 | 0,31 | 0,6034
C:[NM] | 1,4641 | 1 | 1,4641 | 1,80 | 0,2377
D:[H2O2] | 21,2982 | 1 | 21,2982 | 26,15 | 0,0037
AB | 0,2601 | 1 | 0,2601 | 0,32 | 0,5964
AC | 0,0025 | 1 | 0,0025 | 0,00 | 0,9580
AD | 0,255025 | 1 | 0,255025 | 0,31 | 0,5999
BC | 2,80563 | 1 | 2,80563 | 3,44 | 0,1226
BD | 0,64 | 1 | 0,64 | 0,79 | 0,4160
CD | 1,21 | 1 | 1,21 | 1,49 | 0,2773
Error total | 4,07278 | 5 | 0,814555 |  | 
Total (corr.) | 32,859 | 15 |  |  | 
Statistical analysis for response parameter [H2O2]rem (%)
Table 3. Analysis of variance for [H2O2]rem (%)

## Slide 16
Figure 3. Pareto’s diagram for [H2O2]rem (%)

## Slide 17
Figure 4. Surface diagrams for the response [H2O2]rem (%)

## Slide 18
(a)
(b)
(c)
(d)
(e)
(f)
Figure 5. Surface diagrams for combined desirability function

## Slide 19
Factor | Low | High | Optimal
pH | 3.5 | 7.0 | 3.5
[MO] | 50.0 | 200.0 | 200.0
[CAT] | 0.5 | 5.0 | 5.0
[H202] | 0.0685 | 1.0064 | 0.0685
Table 4. Optimal levels for every factor by simultaneous assessment of both response parameters in the CWPO of MO

## Slide 20
Montgomery D.C., (2005). Design and Analysis of Experiments, 6th. ed., John Wiley & Sons, Inc.

## Slide 21: Summary

## Slide 22
Multivariate analysis released main factors affecting CWPO elimination of methyl orange.
MO elimination: [H2O2] > pH X [MO] > [CAT]
[H2O2]rem: [H2O2]
Desirability function allowed proper combination of the responses